Master Specifications for "E-Cast 60”
September 15, 2026

SECTION 042130 - "E-CAST 60"
PART 1 -  GENERAL
1.1 SUMMARY
A. Section Includes:  "E-CAST 60"; cast architectural polymer-modified cement-based units manufactured to simulate the following:

1. Natural cut stone.

2. Terra cotta.
3. Cast iron.

4. Cast stone.

5. Façade ornamentation.

The following may be required for some projects; delete if there are no allowances on the project.
1.2 ALLOWANCES

Retain products and work included in this Section that are covered by cash or quantity allowance. Do not include amounts. Insert descriptions of items in Part 2 or 3 to provide information affecting the cost of the Work that is not included under the allowance. Delete this article if all work is done by lump-sum price.

Remaining paragraphs are examples only; revise to suit Project. Insert additional allowances according to retained types of work and allowances established. If there are multiple drawing designations for types of work, establish separate allowances for each drawing designation.

A. Remove and replace terra cotta as part of terra cotta removal and replacement allowance.

1.3 UNIT PRICES

Do not include amounts. Insert descriptions of items in Part 2 or 3 to provide information affecting the cost of the Work that is not included under the unit price.

Retain this article to establish unit prices during bidding that can be used for unforeseen changes.

Retain this article if using a single Unit-Price Schedule with a column of estimated quantities on which bids are priced and evaluated.

A. Work of this Section is affected by unit prices specified in Division 01 Section "Unit Prices."

1. Unit prices apply to authorized work covered by [quantity allowances] [estimated quantities].

2. Unit prices apply to additions to and deletions from Work as authorized by Change Orders.

1.4 ACTION SUBMITTALS
A. Product Data: For each type of product indicated. Include recommendations for application and use. Include test data substantiating that products comply with requirements.

Retain the following for small projects and where "Micro Cotta" is installed as infill.

B. Shop Drawings: For the following:

1. Scaled drawings showing each distinct "E-CAST 60" unit.

2. Locations of anchors and dimensions of holes and recesses in units required for anchors designed by others.
Retain the following for large or complex projects.

C. Shop Drawings: For the following:

1. Setting number of each new "E-CAST 60" unit and its location on the structure in annotated plans and elevations.

2. Provisions for expansion joints, mortar joints or sealant joints.

3. Provisions for flashing, lighting fixtures, conduits, and weep holes as required.

4. Replacement and repair anchors. Include details of anchors within individual units, with locations of anchors and dimensions of holes and recesses in units required for anchors.

D. Samples for Verification: For the following:

Retain and revise five subparagraphs below and insert others to suit Project.

1. Each type of "E-CAST 60" unit to be used for replacing existing units. Include sets of Samples as necessary to show the full range of shape, color, and texture to be expected.

Retain first subparagraph below and option in second subparagraph for tight control of appearance and unit size (accommodating shrinkage). If retaining, consider limiting this requirement to specific, highly visible units. It will add to Project time and cost.

a. Patterns for "E-CAST 60": Before manufacturing "E-CAST 60" units, submit the actual patterns from which molds will be made for casting new units. Package and ship to prevent loss or damage or make patterns available for inspection by Architect at fabrication plant.

b. For "E-CAST 60," provide one of each shape, color, and texture of unit, suitable and ready for installation.[ Make this submittal after acceptance of patterns for "E-CAST 60."]

2. Sealant Materials: Refer to Division 07 Section "Joint Sealants."

3. Mortar: Provide triplicate cured samples of custom-matched Spec Joint 46 produced with ICE-9 RL admixture, measuring 3/8”w x 4” L and labeled with factory color and sample batch numbers.
4. Accessories: Each type of anchor, accessory, and miscellaneous support.

1.5 QUALITY ASSURANCE
Retain required mockups in first paragraph below; insert others to suit Project. Revise or delete paragraph if test areas were prepared or are required as part of a separate contract.

A. Mockups: Prepare mockups of "E-CAST 60" installation to demonstrate aesthetic effects and set quality standards for materials and execution and for fabrication and installation.

1. Replacement Units: Prepare sample areas not smaller than 48 inches (1200 mm) in least dimension. Erect sample areas in existing walls unless otherwise indicated, to demonstrate quality of materials, workmanship, and blending with existing work. Include a minimum of four "E-CAST 60" units.
a. If sealant joints are required for project, include at least one sealant-filled joint in mockup.
Retain first subparagraph below if mockups are not only for establishing appearance factors.

2. Approval of mockups does not constitute approval of deviations from the Contract Documents contained in mockups unless Architect specifically approves such deviations in writing.

Retain subparagraph below if mockups are installed as part of building rather than erected separately and the intention is to make an exception to the default requirement in Division 01 Section "Quality Requirements" for demolishing and removing mockups when directed unless otherwise indicated.

3. Approved mockups may become part of the completed Work if undisturbed at time of Substantial Completion.

Retain paragraph below if Work of this Section is extensive or complex enough to justify a preinstallation conference.

B. Preinstallation Conference: Conduct conference at [Project site] <Insert location>.

Retain subparagraphs below if additional requirements are necessary; include information about conference.

1. Review methods and procedures related to "E-CAST 60" installation including, but not limited to, the following:

a. Construction schedule. Verify availability of materials, personnel, equipment, and facilities needed to make progress and avoid delays.

b. Materials, material application, sequencing, tolerances, and required clearances.

c. <Insert agenda items>.

1.6 DELIVERY, STORAGE AND HANDLING
A. Deliver "E-CAST 60" components secured to shipping pallets and protected from damage and discoloration.

B. Protect corners from damage. Deliver each piece of "E-CAST 60" with code mark or setting number on unexposed face, corresponding to Shop Drawings, using nonstaining paint.

C. Deliver other materials to Project site in manufacturer's original and unopened containers, labeled with manufacturer's name and type of products.

D. Store "E-CAST 60" components and installation materials in accordance with manufacturer’s instructions.

1. Store "E-CAST 60" components on pallets with non-staining, waterproof covers.

2. Ventilate under cover to prevent condensation.

3. Prevent contact with dirt.

E. Handling:

1. Protect "E-CAST 60" components during handling and installation to prevent chipping, cracking, or other damage.

1.7 PROJECT CONDITIONS

A. Weather Limitations: Proceed with installation only when existing and forecasted weather conditions permit work to be performed according to manufacturers' written instructions and specified requirements.

If required, insert "Extra Materials" Article for extra materials that match products applied or installed.

PART 2 -  PRODUCTS
2.1 E-CAST 60 MASONRY MATERIALS
A. Manufacturer: E-CAST 60 casting mortars and Silquathane 222, Aquaspex 220 and Aquathane UA210 glaze coatings are manufactured by Edison Coatings, Inc., 3 Northwest Drive, Plainville, CT 06062; Phone (860)747-2220. 

B. Fabricator: E-CAST 60 finished castings are produced by Works In Stone, Inc., 8521 Easton Road, Ottsville, PA 18942; Phone:  215-589-9097 
1. Provide new "E-CAST 60" units to match existing deteriorated terra cotta units in physical properties, colors, color variation within units, surface texture, unit profile, and dimensions.

a. Cast Unit Physical Properties:

1) Compressive Strength: 7,000 psi average per ASTM C67 with minimum individual unit strength of 4,500 psi.

2) Compressive Strength: Minimum 7500 psi per ASTM C1013

3) Flexural Strength: 1850 psi at 1” thickness

4) Freeze-Thaw Resistance: No Scaling at 50 cycles per ASTM C666

5) Salt-Scaling Resistance: Rating of “1” at 300 cycles, per ASTM C672

6) Maximum Water Absorption, prior to glaze coating, after 1-hour boiling: Less than 2 percent per ASTM C67.
7) Coefficient of Linear Expansion: Approx. 4 x 10-6 inch/inch/degree F.
b. Glaze Coating Properties:

1) Chemical Resistance: Unaffected by water (7 days), salt water (7 days), proprietary nonionic cleaning solution (2 hours - Edison Coatings E-Wash 30); Softens/recovers Isopropyl alcohol (1 hour); per ASTM D1308

2) Crazing and Cracking Resistance: Min. 100% elongation, min, 500 psi tensile strength, per ASTM D2370.
3) Bond Strength: Minimum 450 psi pull-off adhesion, per ASTM D4541.

4) Shear Bond Strength: Minimum 300 psi per ANSI 118.1

5) Color Stability: dE <2.0, 1000 hours per ASTM G154

2.2 MORTAR MATERIALS
A. Prepackaged mortar shall be SPEC-JOINT 46 Type S (ALT: Type N) as manufactured by Edison Coatings, Inc., Plainville, CT (860) 747-2220. Mortar shall be custom-matched to original mortar unless otherwise specified, including matrix color, aggregate grading and color, and design mix proportions.
1. Portland cement: ASTM C150 Type I, grey or white as required to match original mortar. Fly ash, slag and pozzolans are not permitted as substitutes for Portland cement.

2. Hydrated Lime: ASTM C207 Type S, incorporated as a finely divided powder in uniform particle size, free of lumps, flakes or other inconsistencies.

3. Mortar Aggregate: ASTM C144 Natural sand blend, rounded to sub-angular in shape, washed, screened and dried. Aggregate to be selected to match the color and texture of the original mortar aggregates as closely as possible while remaining in compliance with ASTM C144 grading and soundness requirements.

4. Mortar Colors: Inorganic mineral oxides meeting the requirements of ASTM C797, at levels not to exceed 10% on cement weight, except for carbon black, which may not exceed 2% on cement weight.

5. Admixtures: NO admixtures shall be used without the express written consent of the Architect and the mortar manufacturer. Calcium chloride is not permitted. 
6. Water: No water is to be used. All gaging liquid shall be ICE-9 RL admixture as manufactured by Edison Coatings, Inc., Plainville, CT (860) 747-2220. 
B. All mortar shall be pre-blended, pre-colored and prepackaged under controlled factory conditions. All ingredients are to be batched within plus or minus 1% accuracy, except pigments which shall be weighed to a precision of 0.01%.
C. Mortar shall conform to the minimum property requirements for Type S mortar as given in Table II of ASTM C270, based on 28-day laboratory testing ONLY. 
D. Do not add cement, lime, bonding agents, coloring admixtures, set accelerators, plasticizers, air entraining admixtures or other materials unless specifically authorized in writing.
E. Use of ready-mix mortar (ASTM C1142) is PROHIBITED.
2.3 CLEANING MATERIALS

A. Final cleaning solution shall be E-WASH 30 manufactured by Edison Coatings, a non-ionic, non-toxic, non-corrosive building wash incorporating ingredients from US EPA’s Safer Choice program.
2.4 ACCESSORIES
A. Anchor pins and dowels should be stainless steel. Shelf angles and other similar structural items should be galvanized. Consult Works In Stone for assistance in specifying anchors for the specific application.

B. "E-CAST 60" Anchors: Type and size indicated or, if not indicated, to match existing anchors in size and type. Fabricate anchors from [Type 304] [Type 316] stainless steel.

C. Joint Sealant and Backing: As specified in Division 07 Section "Joint Sealants."
2.5 FABRICATION
A. Shapes: Unless otherwise indicated on Drawings, provide the following:

1. Suitable wash on exterior sills, copings, projecting courses, and components with exposed top surfaces.

2. Drips on projecting components, wherever possible.

3. Replicate exact profile an\d finish of stones submitted to manufacturer for duplication.

B. Tolerances: Fabricate "E-CAST 60" components within specified tolerances.

1. All dimensions: Plus or minus 1/8 inch (3 mm).

2. Maximum Bow, Camber, or Twist: Length/360.

PART 3 -  EXECUTION
3.1 EXAMINATION
A. Examine construction to receive "E-CAST 60" components. Notify Architect if construction is not acceptable. Do not begin installation until unacceptable conditions have been corrected.

3.2 INSTALLATION
A. General: Install "E-CAST 60" components in conjunction with masonry complying with requirements of Division 04 Section "Unit Masonry."
B. Setting:
1. Do not use equipment in a manner that could damage "E-CAST 60" components.

2. Fill dowel holes and anchor slots completely with mortar on non-shrink grout.

3. Point joints with pointing mortar except where sealant-filled joints are specified and indicated on Drawings.

4. Make all joints 3/8 inch (9.5 mm), except as otherwise detailed.

5. Avoid smearing mortar onto the face of the E-CAST 60 units. Sponge face of each unit immediately, if necessary to remove excess setting materials. Do not allow mortar to dry on unit surfaces.

6. Tool joints to a slight concave profile.

7. Do not moist-cure mortar except as may be required under hot weather and low humidity conditions to avoid plastic shrinkage cracking. Do not moist-cure beyond 24 hours.

C. Sealant Joints:

1. Comply with requirements of Division 07 Section "Joint Sealants."
2. Prime ends of "E-CAST 60" components, insert properly sized foam backing rod, and install sealant using sealant gun.

3. Provide sealant joints at following locations and as otherwise detailed:

a. " E-CAST 60" components with exposed tops.

b. Joints at relieving angles.

c. At control and expansion joints.

d. Perimeters open to weather.
3.3 TOLERANCES
A. Installation Tolerances: Comply with manufacturers recommendations, unless otherwise specified.
1. Variation from Plumb: Do not exceed 1/8 inch in 10 feet (3 mm in 3 m) or 1/4 inch in 20 feet (6 mm in 6 m) or more.

2. Variation from Level: Do not exceed 1/8 inch in 10 feet (3 mm in 3 m), 1/4 inch in 20 feet (6 mm in 6 m), or 3/8 inch (9 mm) maximum.

3. Variation in Joint Width: Do not vary joint thickness more than 1/8 inch in 36 inches (3 mm in 900 mm) or 1/4 of nominal joint width, whichever is less.

4. Variation in Plane Between Adjacent Surfaces (Lipping): Do not exceed 1/16‑inch (1.5‑mm) difference between planes of adjacent units or adjacent surfaces indicated to be flush with units.

3.4 ADJUSTING
A. Surface Repair:

1. Repair chipping and other surface damage noticeable when viewed in direct daylight at 10 feet (3 m).
2. Repair with matching touch-up material provided by manufacturer and in accordance with manufacturer’s instructions.

3. Repair methods and results to be approved by Architect and noted on “as-built” drawings for future reference.

3.5 CLEANING
A. In-Progress and Final Cleaning:

1. Clean "E-CAST 60" before sealants are applied, if applicable, and after installed units have cured for a minimum of 10 days.

a. Wet surfaces with water before applying cleaner.

b. Apply cleaner to "E-CAST 60" in accordance with manufacturer’s instructions.

c. Remove cleaner promptly by low-pressure rinsing thoroughly with clean water.

3.6 PROTECTION
A. Protect "E-CAST 60" components from splashing and other damage.
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